SECTION 01 8116

VOC LIMITS FOR ADHESIVES, SEALANTS, PAINTS, AND COATINGS

GENERAL

SUMMARY

This Section includes requirements for volatile organic compound (VOC) limits for adhesives sealants, paints and coatings used for the Project.

Related Sections:

Section 01 8113: “Sustainable Design Requirements”

REFERENCE STANDARDS

General: Comply with the applicable provisions of the referenced standards except as modified by governing codes and the Contract Documents. Where a recommendation or suggestion occurs in the referenced standards, such recommendation or suggestion shall be considered mandatory. In the event of conflict of referenced standards and this specification or within the standards themselves, the more stringent standard or requirement shall govern.

Rule 1168 - "Adhesive and Sealant Applications", South Coast Air Quality Management District (SCAQMD), State of California http://www.aqmd.gov/docs/default-source/rule-book/reg-xi/rule-1168.pdf

Rule 1113 - "Architectural Coatings": South Coast Air Quality Management District (SCAQMD), State of California http://www.aqmd.gov/docs/default-source/rule-book/reg-xi/r1113.pdf

Green Seal Paint Standard GS-11, Green Seal, Inc., Washington, DC. http://www.greenseal.org/Portals/0/Documents/Standards/GS-11/GS-11_Ed3-2_Paints_Coatings_Stains_and_Sealers.pdf

Green Seal Commercial Adhesive Standard GS-36, Green Seal, Inc., Washington, DC http://www.greenseal.org/Portals/0/Documents/Standards/GS-36/GS-36Ed2-1_Adhesives_for_Commercial_Use%202018.pdf

California Air Resources Board (CARB) 2007 https://www.arb.ca.gov/coatings/arch/Approved_2007_SCM.pdf

SUBMITTALS

Manufacturer’s technical information for all interior applied adhesives, sealants, paints and coatings, indicating VOC content in grams/Liter (g/L).

          - Provide product data indicating compliance with General Emissions evaluation and VOC content requirements.

Documentation providing the quantity of each adhesive, sealant, paint, and coating product type used on the Project.

PRODUCTS

INTERIOR ADHESIVES

VOC Limits

The volatile organic compound (VOC) content of all field-applied adhesives, adhesive bonding primers, and adhesive primers used on the interior of this Project shall not exceed the limits defined in Rule 1168 - "Adhesive and Sealant Applications" of the South Coast Air Quality Management District (SCAQMD), of the State of California, with a rule amendment date of October 6, 2017.

The VOC limits defined by SCAQMD are measured in grams per liter (g/L), less water and less exempt compounds.

General: For specified building construction related applications, the allowable VOC content is as follows:

Architectural Applications:

Building Envelope Membrane Adhesive		250

Indoor carpet adhesive						  50

Carpet Pad Adhesive							  50

Wood Flooring Adhesive						100

Rubber Floor Adhesive						  60

Subfloor adhesive							  50

Ceramic Tile Adhesive						  65

VCT and asphalt tile adhesive				  50

Drywall and panel adhesive					  50

Cove base adhesive							  50

Multipurpose construction adhesive			  70

Structural glazing adhesive					100

Specialty Applications:

PVC welding									510

CPVC	welding								490

ABS welding									325

Adhesive primer for plastic					550

Contact Adhesive								  80

Special Purpose Contact Adhesive 			250

Adhesive Primer for Traffic Marking Tape 	150

Structural Wood Member Adhesive 			140

Top and trim adhesive						250

Substrate Specific Applications:

Metal to metal								  30

Plastic foams									  50

Porous material (except wood)				  50

Wood 											  30

Fiberglass									  80

Reinforced Plastic Composite				250

INTERIOR AEROSOL ADHESIVES

VOC Limits

The volatile organic compound (VOC) content of all field-applied aerosol adhesives, used on the interior of this Project shall not exceed the limits defined in the Green Seal standard GS-36, Commercial Adhesives, Edition 2.1, July 12, 2013.  Product specific requirements are as follows:

Aerosol Adhesives

General purpose mist spray						65% VOCs by weight

General purpose web spray						55% VOCs by weight

Special purpose aerosol adhesives				70% VOCs by weight

INTERIOR SEALANTS

VOC Limits

The volatile organic compound (VOC) content of all field-applied adhesives, adhesive bonding primers, and adhesive primers used on the interior of this Project shall not exceed the limits defined in Rule 1168 - "Adhesive and Sealant Applications" of the South Coast Air Quality Management District (SCAQMD), of the State of California.

The VOC limits defined by SCAQMD are as follows. All VOC limits are defined in grams per liter, less water and less exempt compounds.

General: For specified building construction related applications, the allowable VOC content is as follows:

Sealants:

Clear, Paintable, and Immediately

Water-Resistant Sealant 						280

Foam insulation and sealant					250

Grout Sealant									  65

Non-Staining Plumbing Putty				150

Potable Water Sealant						100

Single Ply Roof Membrane Sealants		450

Other Roof Sealants							300

All other Architectural Sealants				250

All other Sealants								420

Sealant Primer:

Architectural - Nonporous 					250

Architectural- Porous 						775

Other 											750

INTERIOR ARCHITECTURAL PAINTS

VOC Limits

The volatile organic compound (VOC) content of all field-applied architectural paints, used on the interior walls and ceilings of this Project shall not exceed the limits defined in the Green Seal standard GS-11, Paints, Edition 3.2, October 26, 2015.  Product specific requirements are as follows:

Paints

Flat											  50

Non-Flat										100

Non-Flat High Gloss Coatings				150

Coatings:

Concrete/Masonry Sealers					100

Fire resistive Coatings						350

Floor coatings								100

Low-Solids Coatings							120

Primers, Sealers, and Undercoaters 		100

Roof Coatings								  50

Rust Preventative Coatings					250

Wood Coatings								275

INTERIOR COATINGS

VOC Limits

The volatile organic compound (VOC) content of all field-applied coating used on the interior of this Project shall not exceed the limits defined in Rule 1113 - "Architectural Coatings" of the South Coast Air Quality Management District (SCAQMD), of the State of California, Amended February 5, 2016.

The VOC limits defined by SCAQMD are measured in grams per liter (g/L), less water and less exempt compounds.

General: For specified building construction related applications, the allowable VOC content is as follows:

Coatings

Building Envelope Coatings					 50

Clear Wood Finish:

Varnish									275

Sanding Sealers						275

Lacquer								275

Concrete-Curing Compounds 				100

Dry Fog Coatings								 50

Floor Coatings 								 50

Low-solids Coatings 							120*

Magnesite Cement Coatings 				450

Primers, Sealers and Undercoaters 			100

Shellac

Clear 									730

Pigmented 								550

Stains 										100

Waterproofing Sealers 						100

Waterproofing Concrete/Masonry Sealers 	100

Wood Preservatives							350

*Note: VOC levels for Low-Solids coatings are measured in grams of VOC per liter of material, including water.

EXECUTION (NOT USED)

END OF SECTION